AMERICOLD MANUFACTURING PROCESS SHEET

| PROCESS DESCRIPTION: ALUMINUM BEARING PLATE MACHINING | PS #: 2111-001 |
| --- | --- |
| DEPARTMENT: 2111 | REV.: 1 |
| PART NAME: BEARING PLATE | DATE: 8-14-95 |
| PART NO.: 59- | PREPARED BY: P. Brandon |
| MACHINE NAME: WASINO BEARING PLATE MACHINE | APPROVED BY: |
| MACHINE NUMBER: 1-0554, 1-0555, 1-0559, 1-0560, 1-0569, 1-0570, 1-0571, 1-0572 | PAGE 1 OF 1 |

- Turn, Face, Bore, First Pass:  Bore Finish to Size and Back Face to Length.

TOOLS REQUIRED

|  | TOOL NUMBER | DESCRIPTION |  |
| --- | --- | --- | --- |
|  | C60-29050 | Turn & Face Tool Holder |  |
|  | C60-29051 | Turn & Face Diamond Cutting Tool |  |
|  | C60-29052 | Boring Bar |  |
|  | C60-29053 | Boring Insert Diamond |  |
|  | C60-29054 | Back Face Bar |  |
|  | C60-29055 | Back Face Carbide Cutting Tool |  |

- SET UP PARAMETERS

SEE ATTACHMENT

| Model: LG-6 W/SR-1 | Workpiece: P/N59-115 | Material: ALUM DIE CAST 380 |
| --- | --- | --- |

| Operation Number | 1 |  |  |  |  | Generation |  | 1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Machining Sequence | 1 | 2 | 3 | 4 |  | Net Cutting Time |  | 16.9 |
| Tool Number | 1 | 2 | 2 | 3 |  | Net Rapid Time |  | 1.7 |
| Machining Operation | FA/TU | 80 | 80 | FA(BACK) |  | Idle Time |  | 10.0 |
| Tool Material | DIAMOND | DIAMOND | DIAMOND | CARB |  | Load / Unload Time |  | 7.0 |
| Spindle RPM | 5488 | 5888 | 6000 | 6000 |  | Transfer Time |  |  |
| Surface Feet/Min. | 2280 | 1178 | 1178 | 1371 |  | Total |  | 35.6 |
| Depth of Cut | 0.02 | 0.04 | 0.01 | 0.02 |  |  |  |  |
| Feed Inch/Rev. | 0.004 | 0.01 | 0.0025 | 0.002 |  |  |  |  |
| Length of Cut | 1.62 | 203 | 2.3 | 0.17 |  |  |  |  |
| Cutting Time sec. | 4.9 | 2.3 | 9.2 | 8.9 |  |  |  |  |
| Rapid Traverse Time Sec. | 0.8 | 0.3 | 0.3 | 0.3 |  |  |  |  |
| Remarks |  | ROUGH | FINISH | = GAIN 35.6 SEC |  |  |  |  |

ABBREVIATIONS:		BO	Bore		CE	Center		CH	Chaster

CU	Cutoff		DR	Drill		FA	Face

GR	Groove	MI	Mill		RE	Ream

TA	Tap		TH	Thread		TU	Turn

PU	Pusher		BF	Barfeed

Idle Time includes (but is not limited to): Tool Change Time, Positioning Time, Spindle Start and Stop Time and Dwells.

NOTE:  THIS IS AN ESTIMATE ONLY:  Cutting parameters are based on data contained in the MACHINING DATA HANDBOOK 3rd edition, reflecting options conditions.  This time estimate